## Slide 1
Redox flow batteries for grid-scale
energy storage
Vijay K. Ramani
Roma B. and Raymond H. Wittcoff Distinguished University Professor
Washington University in St. Louis

## Slide 2
Overview
Requirements of large-scale energy storage systems
The electrode-decoupled redox flow battery (ED-RFB)
  Development of highly selective separators
  Formulation of the electrolytes
Performance of a model electrode-decoupled RFB
Conclusion

## Slide 3
The energy storage ideal
http://www.newkirk-electric.com/projects/power-generation/ludington-hydroelectric-pumped-storage-dam/8
https://energyhub.theiet.org/users/57714-anthony-price/posts/18914-energy-storage-opportunities-and-trends
https://depts.washington.edu/maple/
The ideal energy storage system is -
Cheap (< $50/KWh DOE target)
Widely deployable
Available 24/7
Dischargeable at multiple time scales and current rates

## Slide 4
Separator
Load or power source
e-
e-
Electrolyte
What is a flow battery?
Au plated
current collector
Au plated
current collector
VO2++ 2H+ + e- ↔ VO2+ + H2O (+1V vs. SHE)
V3++ e- ↔ V2+
(-0.26V vs. SHE)
ions
ions

## Slide 5
Advantages of a RFB
Power (KW)
Energy (KWh)
Conventional battery design line
Redox flow battery
design space
Operational duration =
Energy/Power (h)
System cost ($/KWh)
Conventional batteries
Redox flow batteries
Energy and power are decoupled => greater design flexibility => lower scale-up costs

## Slide 6
A brief history of Redox flow batteries
1955 – A.M Posner – An Fe-Sn and Br-Sn “redox fuel cell”
1975-77 – NASA – Fe-Ti RFBs
1977-89 – NASA – Fe-Cr RFBs
1984 – Maria Skyllas-Kazacos – Practical demonstration of a VRFB
1999 onwards – Plurion / Frank Walsh (U. Southampton) – Zn-Ce RFB
Several other inorganic and organic based RFB chemistries have been proposed and are in various stages of commercialization
The most famous - The all-V redox flow battery

## Slide 7
An electrode-decoupled (ED-)RFB
Design flexibility – greater variety of actives
Tunable cell voltage
Can lead to capacity fade due to mixing
Some designs require phase change (deposition/dissolution) of one or more actives
Our system is all-soluble, electrode-decoupled and long lasting

## Slide 8
Highly permselective membrane
developed
Made at 100cm2 and beyond
Highly selective
Extremely stable in ED-RFB actives
Low Area specific resistance (ASR)

## Slide 9
Part 2-
Survey of potential aqueous
electrolytes

## Slide 10
Selection of RFB couples
Selection criteria:
No H2 evolution
>=1V cell
No plating processes on either electrode
Preferably benign (non-toxic, no side reactions)
H+/H2
0.00V
V3+/V2+
-0.26V
Cr3+/Cr2+
-0.42V
Vi4+/Vi3+
-0.36V
Fc2+/Fc+
0.39V
I3-/I-
0.53V
Fe3+/Fe2+
0.77V
V5+/V4+
1.00V
Br/Br-
1.08V
Ce4+/Ce3+
1.61V
Zn2+/Zn
-0.76V
TiO2+/Ti3+
0.19V

## Slide 11
Economic criterion for ED-RFB actives selection
Estimated for a 80% efficient 2GW/10GWh system
Actives cost only – balance of plant should add up to <$100/KWh
All-V and V-Ce are out of the price range!
Novel systems needed – Ti-Ce is promising, earth-abundant and potentially problem free
Ti
Ce
https://pubs.usgs.gov/fs/2002/fs087-02/

## Slide 12
Schematic of a typical Ti-Ce ED-RFB
Electrode-decoupled using an AEM separator – quaternized cardo-polyether ketone (QPEKC) functionalized with trimethylamine (TMA)

## Slide 13
Part 3-
The Ti-Ce electrode-decoupled
redox flow battery

## Slide 14
Schematic of a typical Ti-Ce ED-RFB
Electrode-decoupled using an AEM separator – quaternized cardo-polyether ketone (QPEKC) functionalized with trimethylamine (TMA)

## Slide 15
Performance of a Ti-Ce ED-RFB
Use of AEM improves RFB performance compared to Nafion 117

## Slide 16
Conclusions
The potential of suitably structured AEMs to deliver ED-RFBs with elemental actives is demonstrated.
Ti-Ce shown to be a very cost competitive (better than Fe-Cr) ED-RFB without the problems of the Fe-Cr system.
Choice of counter-ion/supporting electrolyte plays a key role in cell performance and cost.
The road to low cost, long-term energy storage in ED-RFB runs through low cost, fairly dense electrolytes

## Slide 17
Acknowledgements
This study was funded by the Advanced Research Projects Agency – Energy (ARPA-E) of the U.S Department of Energy through grant number DE-AR0000768.
The cost model described here was developed by Borealis Technology Solutions LLC (Mr. Thomas Gregory) using inputs provided by WUSTL under a consulting contract.